## Slide 1: International Perforating Symposium (IPS) 2016
Thermal Decomposition Progress with HMX Explosives

## Slide 2
Thermal Decomposition Progress with HMX Explosives
AGENDA/INTRODUCTION
Review previous work (SPE 174209)
Update on API budget and LLNL testing
Detailed results on Perforating Gun/HMX Charge tests
Review of plans for continued work
IPS 16-02

## Slide 3
Thermal Decomposition Progress with HMX Explosives
Perforating System
Components
IPS 16-02
Perforating Gun
Detonating Cord
Shaped Charge
Arming Sub
Detonator – Det Cord Connection
Perforating Gun
Bottom/Toe
Detonators
Detonating Cord
Shaped Charges
Time Delays
Bi-directional boosters

## Slide 4
Thermal Decomposition Progress with HMX Explosives
Thermal Decomp. Effects
IPS 16-02
Based on time temperature plot provided by manufacturer, HNS was selected over HMX
Result: 30-40% reduction in penetration and an estimated 20% reduction in well performance
180 bbl/day
298 bbl/day
HMX
HNS
Performance/Economics

## Slide 5
Thermal Decomposition Progress with HMX Explosives
Time-Temp Curve
IPS 16-02
Single limit based on explosive type
Does not indicate performance degradation

## Slide 6
Thermal Decomposition Progress with HMX Explosives
Thermal Decomp. Effects
Safety
IPS 16-02
Consequence
Increasing Time and Temperature Exposure

## Slide 7
Thermal Decomposition Progress with HMX Explosives
Balancing Safety and Performance
IPS 16-02
Time
Temperature
Critical Temp
Performance Limit
Thermal Stability Limit
Performance Degradation
Thermal Runaway &
Explosion
Performance Loss
Thermally Stable -Unaffected Performance
Theoretical improved Time-Temp curve with degrading performance loss as the critical temperature is approached.

## Slide 8
Thermal Decomposition Progress with HMX Explosives
Previous Work (SPE 174209)
IPS 16-02
Thermal decomposition of explosives can have significant impact on well productivity and safety
Existing time-temperature curves used for explosive selection
  May be inaccurate over long extrapolations
  Use poorly qualified materials and test setup
  Do not provide all of the information needed to select explosives
Common thermal stability tests
  Do not reflect configuration of explosives in perforating systems
  Do not relate safety and performance
  Measure different aspects of thermal decomposition
Conclusions

## Slide 9
Thermal Decomposition Progress with HMX Explosives
Previous Work (SPE 174209)
IPS 16-02
Immediate
Explosive components testing at manufacturer
Medium Term
Laboratory testing at Lawrence Livermore National Lab with API support
Longer time duration ODTX tests with explosive material from industry relevant blends
Long Term
Scalable model to provide performance and safety guidance for industry through additional testing
Explosive materials
Assess accuracy of existing curves
Identify critical components (i.e. shaped charge, booster, det cord, etc.)
Individual components
Full system testing
Forward Plan

## Slide 10
Thermal Decomposition Progress with HMX Explosives
ODTX Test
Safety Test – info on time and temperature at which explosion will occur
Instantaneous exposure to temperature
IPS 16-02

## Slide 11
Thermal Decomposition Progress with HMX Explosives
Extrapolations from Lab Tests
IPS 16-02
Logarithmic Time Scale
Non-Logarithmic Time Scale

## Slide 12
Thermal Decomposition Progress with HMX Explosives
ODTX vs. Downhole Conditions
Simple Test
Basis for current curves
Amount of historical tests
Potential for fundamental thermal decomposition model (instead of empirical)
IPS 16-02
Safety only – no performance
Instantaneous exposure temperature dissimilar to downhole exposure
Spherical heat boundary
Benefits
Disadvantages

## Slide 13
Thermal Decomposition Progress with HMX Explosives
Key Questions to Answer
Where do actual explosive devices fall on the existing time-temp curves?
Do oilfield explosive powders behave the same as previously tested powders (ODTX)
How do ODTX experiments compare to downhole exposure conditions?
IPS 16-02
Compare device tests to curves
Compare ODTX tests using oilfield powders with previous tests
Compare device tests with ODTX experiments

## Slide 14
Thermal Decomposition Progress with HMX Explosives
Path
IPS 16-02
API Approved $150k for Thermal Decomposition study (2016)
Explosive Device Testing
  Initial focus on HMX
  Initial work completed for Shaped Charges
ODTX Testing (LLNL)
  LLNL Phase 1: Shaped Charge Booster
  LLNL Phase 2: Shaped Charge Main
  API & LLNL negotiating contract – expected to begin Phase 1 in Q2

## Slide 15
Thermal Decomposition Progress with HMX Explosives
Plan
Reserve batches of HMX used in shaped charges
  Booster – pure, fine HMX
  Main – desensitized HMX
Build shaped charges for thermal decomposition experiments under simulated downhole conditions
Supply HMX powders of the same batch for ODTX experiments
IPS 16-02

## Slide 16
Thermal Decomposition Progress with HMX Explosives
Device Testing
Simulating Downhole Conditions
Temperature Exposure: ~1 hr ramp to temp.
Test Conditions:
  Loaded in perforating gun (comparable free volume)
  Sealed perforating gun
  Heat applied externally to perforating gun (comparable to downhole exposure)
IPS 16-02

## Slide 17
Thermal Decomposition Progress with HMX Explosives
Shaped Charge Test Program
Thermal exposure
  Pre-heat to ~30°F of set temperature (prevent overshoot)
  Target temperatures: 345°F, 365°F, 385°F, 400°F
Test stop conditions
  Thermal event occurs (indicated by temperature measurement)
  Significant time lapse with no thermal event
Conduct standard QC with any remaining shaped charges
IPS 16-02

## Slide 18
Thermal Decomposition Progress with HMX Explosives
Shaped Charge Test Program
IPS 16-02
Charge Temperature 1 – data acq.
Charge Temperature 2 – data acq.
Charge Temperature 3 – controller

## Slide 19
Thermal Decomposition Progress with HMX Explosives
Shaped Charge Test Program
IPS 16-02
Charge Thermocouples
Heat Tape/Cable
Electronic Pressure Relief Solenoid
3-3/8” 4SPF 0 Degree Perforating Gun
19g HMX DP Charges

## Slide 20
Thermal Decomposition Progress with HMX Explosives
Results
IPS 16-02
Summary
Target Temp. | Total Time | Results
345°F | 61 hrs | All 4 charges ok
365°F | 62 hrs | 1 charge deflagrated (12.5 hrs) 3 charges ok
385°F | 14.7 hrs | 1 charge 10% decomp., 5 in. penetration 3 charges ok
400°F | 7.1 hrs* | 1 charge partially jetted 3 charges deflagrated*

## Slide 21
Thermal Decomposition Progress with HMX Explosives
Results
400°F
IPS 16-02
Chart: 400°F Temperature Test
Temperature spike from thermal event
Thermal couples damaged, not reading
Note: Controlling thermocouple expelled from gun, undamaged. Temperature control lost. Remaining charges exposed to ~500°F.

## Slide 22
Thermal Decomposition Progress with HMX Explosives
Results
IPS 16-02
Chart: Max. Exposure Time, hours
| 2 | 2 | 3 | 3 | 4 | 4 | 5 | 5 | 6 | 6 | 7 | 7 | 8 | 8 | 9 | 9 | 24 | 24 | 48 | 48 | 200 | 200 | 300 | 300 | 400 | 400 | 500 | 500 | 600 | 600 | 700 | 700 | 800 | 800 | 900 | 900
vert | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700
labels1 | 580 | 580 | 580 | 580 | 640
horiz | 200 | 200 | 300 | 300 | 400 | 400 | 500 | 500 | 600 | 600
400 Fire | 400
hmxhc | 400 | 285
385 | 385
vert | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700 | 100 | 700
labels1 | 580 | 580 | 580 | 580 | 640
horiz | 200 | 200 | 300 | 300 | 400 | 400 | 500 | 500 | 600 | 600
400 Fire | 400
hmxhc | 400 | 285
 | 365 | 365
Unpredictable outcome when existing curve is exceeded
Severity of event appears to increase with temperature
No reactions caused ruptures in the perforating gun (although these results could be different in a full explosive train).

## Slide 23
Thermal Decomposition Progress with HMX Explosives
Discussion
Data is applicable to shaped charges only
Reminder: Initiation is a statistical event (i.e. 1 out 4 @ 365°F)
Other explosive components likely behave differently
More severe reactions such as Deflagration to Detonation Transitions may occur in full perforating systems with other more sensitive components in the explosive train
IPS 16-02

## Slide 24
Thermal Decomposition Progress with HMX Explosives
Secondary Results
Performance Data
IPS 16-02
Exposure time significantly beyond predicted value
Performance may decrease under long over-exposure even without full decomposition
  Further testing is required to understand the effects of exposure time at a given temperature
  Testing should evaluate performance at short and long exposure times
Unclear transition between performance loss and total degradation
Chart: Temperature Exposure Effects on Penetration
| 75 | 345 | 365 | 385
T.T.P (in) | 43.75 | 32.75 | 37.1667 | 31.6667

## Slide 25
Thermal Decomposition Progress with HMX Explosives
Refined Theoretical Curve
IPS 16-02
Temperature
Time
Thermally Stable –
Unaffected Performance
Thermal Runaway & Explosion
Performance Loss
Performance Degradation
Original
Refined

## Slide 26
Thermal Decomposition Progress with HMX Explosives
Closing Remarks & Continued Work
Premature to draw conclusions from results – existing time-temperature curves should continue to be used!
Expand test range to +400°F and 200+ hours
Compare results with ODTX tests from LLNL
Evaluate exposure time effects on performance
Expand testing to other explosive components
Expand testing to full system for interactions
IPS 16-02